## Slide 1: Terminology
Revision – 2022-09-31

## Slide 2: Steps of Wood Finishing
A Clear and Stain Finish System
  Sand
  Stain
  Sealer
  Sand
  Shade and or Glaze (optional)
  Topcoat
  Sand
  Topcoat

## Slide 3: Steps of Wood Finishing
A Typical Pigmented System
  Sand
  Primer / Sealer
  Sand
  Topcoat
  Sand
  Topcoat

## Slide 4
Choose a Coating System
  Clear or Pigmented
  Stain or Natural under a Clear?
  To Glaze, or Not to Glaze?
  What Level of Durability
  What Price Point
  Environmental Considerations – HAP’s VOC’s
  Application Considerations
    Minimum Application Temperature
    Special Equipment Required
    Dust and Airborne Debris
Steps of Wood Finishing

## Slide 5
Atomization
Steps of Wood Finishing

## Slide 6
  Conventional Air Spray - (Cup, Pump or Pressure Pot)
  HVLP Air Spray - (Cup, Pump or Pressure Pot)
  Compliant Air Spray - (Cup, Pump or Pressure Pot)
  HVLP Turbine
  Air Assisted Airless (HVLP or Not)
Steps of Wood Finishing
How do we Atomize a Coating?

## Slide 7
  Airless
  Electrostatic
  Roll Coater
  Curtain Coater
  Flow Coater
  Vacuum Coater
  Automated Application Devises and Robots
Steps of Wood Finishing
How do we Atomize a Coating?

## Slide 8
  Fluid Tip Size
    Thicker the material, the bigger the tip
    The bigger the tip, the greater the flow rate
  Operating Pressure(s) - Energy
    Thicker the material the higher the energy required for atomization
  Flow Rate
    Greater flow requires more energy
Steps of Wood Finishing
How do we Atomize a Coating?

## Slide 9
  Spray Booth
  Air Make Up System
  Dust Control
  Environmental Controls (Heat and AC)
  Compressed Air System
    Adequate Volume?
    Clean?
    Dry?
Steps of Wood Finishing
Setting Up a Spray Environment

## Slide 10
Components of a Coating

## Slide 11
Solvent
  Dissolves resins and reduces viscosity
  Solvent is many different chemicals
  Controls flow, level and dry
  Evaporates out of the coating
Resin
  Alkyd, Amino, Acrylic, Polyester, Epoxy, Urethane, Vinyl, Nitrocellulose
Pigment
  Titanium Dioxide, Industrial Colorants
Additives and Extenders
  Calcium Carbonate, Talc, Micronized Silica, Wax
What’s in a Can?

## Slide 12
Solvent vs. Water Borne

## Slide 13
Wet Film Build

## Slide 14
Wet Film Build

## Slide 15
Typical wood coating application – 3 to 5 wet mils
Coating
Substrate
Wet Film Build

## Slide 16
Wet Film Build

## Slide 17
Dry Film Build

## Slide 18
Solid Portion of a coating contains all film forming components
Volatile or solvent portion is a vehicle to carry film formers and does not remain in the film
Solid portion is typically heavier than the solvent portion
Solvent Portion
Solid Portion
50% VS
60% WS
50% VV
40% WV
128 Fluid Ounces
64 Fluid Ounces
64 Fluid Ounces
Volume and Weight Solids
Dry Film Build

## Slide 19
Solvent
  Dissolves resins and reduces viscosity
  Solvent is many different chemicals
  Controls flow, level and dry
  Evaporates out of the coating
Resin (Solids)
  Alkyd, Amino, Acrylic, Polyester, Epoxy, Urethane, Vinyl, Nitrocellulose
Pigment (Solids)
  Titanium Dioxide, Industrial Colorants
Additives and Extenders (Solids)
  Calcium Carbonate, Talc, Micronized Silica, Wax
Dry Film Build

## Slide 20
Typical wood coating application – 3 to 5 dry mils
Dry Film Build

## Slide 21
Mix Well Before Use

## Slide 22
Mix Well

## Slide 23
Viscosity

## Slide 24
Large Wet Particles – Many Air Voids
Resulting in Bubbles
Entrapped Air
Viscosity

## Slide 25
Orange Peel
Viscosity

## Slide 26
Bubble Cavities
Viscosity

## Slide 27
Micro Bubbles
Viscosity

## Slide 28
Smaller Wet Particles – Less Entrapped Air
Fewer Bubbles
Viscosity

## Slide 29
Pigmented coatings are shipped at high viscosity to prevent settling – reduction is usually required
Viscosity
Why don’t we ship all products to the right viscosity?

## Slide 30
Learn to measure viscosity properly.
Good Starting Point – 25” to 30” in a Ford #4
Viscosity
What is the correct viscosity for a product?

## Slide 31
Adding solvent will decrease viscosity
Viscosity
How do you lower viscosity?

## Slide 32
Solvent Portion
Solid Portion
50% VS
50% VV
64 Fluid Ounces
64 Fluid Ounces
Adding Solvent to Lower Viscosity
Viscosity
Solvent Portion
Solid Portion
70.4 Fluid Ounces
64 Fluid Ounces
Before Solvent
After 5% Solvent
48% VS
52% VV

## Slide 33
The percentage of solids in a coating?
Flow and leveling?
The dry thickness of a coating?
Open time?
Viscosity
How will lowering viscosity affect -

## Slide 34
Open Time

## Slide 35
Open time to short = poor flow and leveling
Open time adequate = good flow and leveling
Wet edge
How long the coating stays wet
Open Time

## Slide 36: What Influences Open Time?
Coating formulation
Coating solids
Wet film build
Application equipment
Ambient temperature
Relative humidity
Substrate temperature
Material temperature
Open Time

## Slide 37: Control the Variables
Building Engineering Controls
  Ambient temperature and humidity
  Air flow
Automation
  Automated sprayers control wet film thickness
  Standardize application equipment – pumps – spray heads
Force Drying
  IR pre-heaters control substrate temperature
  In-line fluid heaters control coating temperature
  Force drying systems control flash-off, drying and curing temperatures
  Influences dry to touch, sand and stack times
Open Time

## Slide 38
How do you increase open time?
Which one do you use?
Why not different coatings for different climates?
Open Time

## Slide 39
Solvent Portion
Solid Portion
50% VS
50% VV
64 Fluid Ounces
64 Fluid Ounces
Adding Solvent to Increase Open Time
Open Time
Solvent Portion
Solid Portion
70.4 Fluid Ounces
64 Fluid Ounces
Before Solvent
After 5% Solvent
48% VS
52% VV

## Slide 40
Solvent Portion
Solid Portion
50% VS
50% VV
64 Fluid Ounces
64 Fluid Ounces
Adding Solvent to Increase Open Time & Viscosity
Open Time & Viscosity
Solvent Portion
Solid Portion
76.8 Fluid Ounces
64 Fluid Ounces
Before Solvent
After 5% Thinner & 5% Retarder
46% VS
54% VV

## Slide 41
Grain Raise

## Slide 42
Reaction of wood to water
Wood fibers on the surface swell and rise up when saturated with water
Not as pronounced with solvent borne coatings
How can we avoid it?
Grain Raise

## Slide 43
VOC

## Slide 44
http://www.epa.gov/oar/oaqps/gooduphigh/chartsn.gif
VOC + NOx + Heat + Sunlight = Ozone

## Slide 45: Federal Regulations
Congress created the 1970 Clean Air Act (CAA)
This act authorized the EPA to regulate VOC emissions on specific industries
For example – A certain area of the country may limit the VOC content of a coating to 670 grams/liter

## Slide 46
Solvent
NC Lacquer
Solids
VOC Content
725 grams/liter
5.75 lbs/gallon
WPG 7.60 lbs/gal
17% Vol. Solids
83% Solvent
EPA Reg.
670 grams/liter
5.60 lbs/gallon

## Slide 48
Solvent
KlearVar
Solids
VOC Content
551 grams/liter
4.6 lbs/gallon
WPG 7.91 lbs/gal
32% Vol. Solids
68% Solvent
EPA Reg.
670 grams/liter
5.60 lbs/gallon

## Slide 49
HAP’s

## Slide 50: Federal Regulations
Congress created the 1970 Clean Air Act (CAA)
Congress amended the CAA in 1990 to include 189 HAP’s
This act authorized the EPA to regulate HAP’s emissions on specific industries

## Slide 51
189 Hazardous Air Pollutants

## Slide 52
189 Hazardous Air Pollutants

## Slide 53
Solvent
Any Brand Lacquer
Solids
HAPs Content
Solvents
Solids
Toluene – Xylene - MEK
Dibutyl Phthalate

## Slide 54
Green Organizations

## Slide 58
WWW.MLCAMPBELL.COM
Darrel Young
Training Manager
ML Campbell Wood Finishing Systems
darrel.s.young@mlcampbell.com